Ukrgazifikatsia-Yug

PE 80 Water pipes

Pipes are produced according to TU U V.2.7-21547843.006-2001 for water pipelines also for drinking-water supply and other liquid or gaseous substances, to which polythene chemically stable.

| Оutside diameter | MAXIMUM WATER WORKING PRESSURE, MPa |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 2,5 |  |  | 2,0 |  |  | 1,6 |  |  | 1,25 |  |  |
|  | SDR 6 |  |  | SDR 7,4 |  |  | SDR 9 |  |  | SDR 11 |  |  |
|  | Wall thickness | Weight 1 m/r | Price, $ | Wall thickness | Weight 1 m/r | Price, $ | Wall thickness | Weight 1 m/r | Price, $ | Wall thickness | Weight 1 m/r | Price, $ |
| 25 | 4,2 | 0,281 | 1,01 | 3,5 | 0,243 | 0,87 | 3,0 | 0,214 | 0,77 | 2,3 | 0,173 | 0,70 |
| 32 | 5,4 | 0,457 | 1,64 | 4,4 | 0,389 | 1,40 | 3,6 | 0,330 | 1,19 | 3,0 | 0,282 | 1,03 |
| 40 | 6,7 | 0,709 | 2,55 | 5,5 | 0,608 | 2,19 | 4,5 | 0,516 | 1,86 | 3,7 | 0,437 | 1,60 |
| 50 | 8,3 | 1,096 | 3,95 | 6,9 | 0,945 | 3,40 | 5,6 | 0,797 | 2,99 | 4,6 | 0,674 | 2,45 |
| 63 | 10,5 | 1,737 | 6,25 | 8,6 | 1,482 | 5,34 | 7,1 | 1,268 | 4,60 | 5,8 | 1,062 | 3,84 |
| 75 | 12,5 | 2,747 | 9,89 | 10,3 | 2,397 | 8,63 | 8,4 | 2,068 | 7,44 | 6,8 | 1,769 | 6,37 |
| 90 | 15,0 | 3,546 | 12,77 | 12,3 | 3,026 | 10,89 | 10,1 | 2,571 | 9,45 | 8,2 | 2,150 | 7,94 |
| 110 | 18,3 | 5,279 | 19,00 | 15,1 | 4,532 | 16,32 | 12,3 | 3,819 | 14,15 | 10,0 | 3,187 | 11,87 |
| 160 | 26,6 | 11,145 | 40,12 | 21,9 | 9,536 | 34,33 | 17,9 | 8,056 | 30,00 | 14,6 | 6,762 | 25,43 |
| 225 | 37,4 | 22,027 | 79,30 | 30,8 | 18,850 | 69,86 | 25,2 | 15,952 | 59,43 | 20,5 | 13,341 | 50,23 |
| 315 | 52,3 | 43,104 | 160,17 | 43,1 | 36,925 | 146,13 | 35,2 | 31,166 | 124,00 | 28,6 | 26,028 | 104,10 |
| 400 | --- | --- | --- | 54,7 | 59,463 | 248,34 | 44,7 | 50,208 | 198,79 | 36,3 | 41,944 | 176,98 |
| 500 | --- | --- | --- | --- | --- | --- | 55,8 | 78,336 | 322,01 | 45,4 | 65,538 | 273,94 |
| 630 | --- | --- | --- | --- | --- | --- | --- | --- | --- | 57,2 | 104,034 | 440,02 |

| Оutside diameter | MAXIMUM WATER WORKING PRESSURE, MPa |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1,0 |  |  | 0,8 |  |  | 0,6 |  |  | 0,5 |  |  |
|  | SDR 13,6 |  |  | SDR 17 |  |  | SDR 21 |  |  | SDR 26 |  |  |
|  | Wall thickness | Weight 1 m/r | Price, $ | Wall thickness | Weight 1 m/r | Price, $ | Wall thickness | Weight 1 m/r | Price, $ | Wall thickness | Weight 1 m/r | Price, $ |
| 25 | 2,0 | 0,152 | 0,52 | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 32 | 2,4 | 0,235 | 0,77 | 2,0 | 0,199 | 0,68 | --- | --- | --- | --- | --- | --- |
| 40 | 3,0 | 0,368 | 1,20 | 2,4 | 0,302 | 1,09 | 2,0 | 0,255 | 0,94 | --- | --- | --- |
| 50 | 3,7 | 0,558 | 1,80 | 3,0 | 0,462 | 1,59 | 2,4 | 0,383 | 1,38 | 2,0 | 0,322 | 1,16 |
| 63 | 4,7 | 0,884 | 2,82 | 3,8 | 0,731 | 2,63 | 3,0 | 0,590 | 2,18 | 2,5 | 0,504 | 1,81 |
| 75 | 5,6 | 1,539 | 4,74 | 4,5 | 1,318 | 4,11 | 3,6 | 1,130 | 3,87 | 2,9 | 0,978 | 3,52 |
| 90 | 6,7 | 1,796 | 5,82 | 5,4 | 1,485 | 5,35 | 4,3 | 1,212 | 4,36 | 3,5 | 1,005 | 3,62 |
| 110 | 8,1 | 2,659 | 8,62 | 6,6 | 2,208 | 7,95 | 5,3 | 1,816 | 6,74 | 4,2 | 1,474 | 5,71 |
| 160 | 11,8 | 5,599 | 19,16 | 9,5 | 4,615 | 16,61 | 7,7 | 3,811 | 12,97 | 6,2 | 3,14 | 11,70 |
| 225 | 16,6 | 11,067 | 37,60 | 13,4 | 9,135 | 32,89 | 10,8 | 7,499 | 25,44 | 8,6 | 6,096 | 22,35 |
| 315 | 23,2 | 21,638 | 74,17 | 18,7 | 17,800 | 64,08 | 15,0 | 14,549 | 49,60 | 12,1 | 11,986 | 43,15 |
| 400 | 29,4 | 34,789 | 125,84 | 23,7 | 28,630 | 109,07 | 19,1 | 23,549 | 84,62 | 15,3 | 19,209 | 73,15 |
| 500 | 36,8 | 54,374 | 197,15 | 29,7 | 44,817 | 167,34 | 23,9 | 36,745 | 132,28 | 19,1 | 29,963 | 111,87 |
| 630 | 46,3 | 86,235 | 346,06 | 37,4 | 71,119 | 276,03 | 30,0 | 58,110 | 229,16 | 24,1 | 47,597 | 179,35 |

The pipes are manufactured to the highest standards and pass all complex of researches, have the hygienic certificate of Ministry of Health of Ukraine.

Str. Ilfa and Petrova, Odessa, 65104, Ukraine, E-mail: ukrgaz-yug@yandex.ru

Web-page:    http://www.trubype.com.ua Тел./факс: (048) 746-79-98 Тел.: (048) 746-91-03

Settlement account 2600531331  UkrGasBank in Odessa, MFO 328588, Code EDRPOU 20972455